[image: image5.wmf] 

 

                                                                

                          

 

Messrs:

 

 

 

ZAK

 

For the coming season:

 

   

2006 / 2007

 

QUALITY SERVICE

 

you have chosen our art.:

 

 

 

FIRMA WINDTEX VELURE

  

 

In order to ascertain if our fabrics characteristics meet your specifications we enclose the following data:

 

Characteristics:

 

Data:

 

Testin

g method:

 

1.  

Structural Characteristics

 

 

 

 

 

 

 

 

                       Material         Fiber

 

1.1.      

Weight sqm

 

gr. 22

0 +/

-

 10%

 

FIRMA

 

100

%PES

 

WINDTEX

 

 

100%PU

 

1.2.

 

Composition

 

 

82

%PES 

1

8

%

 

PU

 

VELURE

 

 

 

100

%PES

 

1.3.      Minimum useable width

 

140  

-

 145

 

 

 

 

2.         

Mechanical and Physical Performance

             Warp

 

 

             

Weft

 

 

 

 

2.1  Dimensional stability after washing  40°C

 

  

 

    

+/

 

-

2%

 

  

 

   

+/

 

-

2%

 

 

UNI 

–

 9294

 

2.2  Abrasion resistance: Martindale machine

 

  34

.000 loop  Starting 

Breaking Knit         (9Kpa)

 

BS 5690

 

2.3  Pilling: Martindale method

 

 estimation  5

 

 

 

 

 A 2.000 cicli

 

UNI E15.12.434.0

 

2.4   Waterproofness:

 

 10.000 mm

 

 

 

 

 

 

 

EN 

–

 20811

 

2.5 

  

Water vapour transmission

 

  <10

 m² Pa/W

 

 

 

 

 

 

ISO 31092

 

3.          

Care instruc

tions

 

     

   

    

    

      

 

3.1

 

        

Recommended print temperature not over 205°     

–

     Time 40 seconds    

–

     Pressure 4 bars

 

4.          

Colour Fastness to: (black colour)

 

 

 

 

 

 

 

 

 

 

 

 

 

 

 

 

 

 

4.1.1.     Wet Rubbing

 

Index

 

>4

 

 

 

 

 

 

 

 

ISO 105 

–

X12

 

4.1.2.     Dry Rubbing

 

Index

 

>4

 

 

 

 

 

 

 

 

ISO 105 

–

X12

 

 

 

D

e

terioration

 

 

 

Stain

 

 

 

 

 

 

WO

 

P

C

 

PES

 

PA

 

CO

 

AC

 

 

4.2.1.      Acid perspiration

 

>4

 

>4

 

>4

 

>4

 

>4

 

>4

 

>4

 

ISO 105 

–

E04

 

4.2.2.      Alkaline perspiration

 

>4

 

>4

 

>4

 

>4

 

>4

 

>4

 

>4

 

ISO 105 

–

E04

 

4.3.       

 

 

Water

 

>4

 

>4

 

>4

 

>4

 

>4

 

>4

 

>4

 

ISO 105 

–

E01

 

 

 

 

 

 

 

 

 

 

Colognola ai Colli, 

1

st

 december

 2006

 

    

                         

 

                       __

__                           

 

 

 

 

   ____

___

 

                               

Quality control                                                                            

                           Quality direction

 

                

 

 

 

 

In order to improbe the product we riserve to  introduce changes if necessary.

                            

 

 

41

-

MOD

-

SPRO

-

REV

ø

 




1 dicembre 2006

[image: image1.png](/
AGOTEX..

TESSUTI INNOVATIVI PER LA CALZATURA
E L'ABBIGLIAMENTO SPORTIVO










	[image: image2.png]ACCOPPIATO

®

di QUALITA



[image: image3.png]



	_______________________________________________________________________________________

VAGOTEX WINDTEX S.p.a

Viale del Lavoro, 15 – 37030 Colognola ai Colli – Verona

Tel. 045 6159111 – Fax 045 6152060 – 045 6172504

Cod. Fisc. e Part. IVA 00895500239 – Reg. impr. di VR n.12221 – Capitale Sociale € 775.000

www.vagotex.it     info@vagotex.it    www.windtex.it 
	[image: image4.png]CERTITEX

ERTICALL

AZIENDA CON SSTIMA'

GESTIONE QUALITA
‘CONPORME ALLA NORMA UNI EN 150 9001:2000
"CIRTIACATI N 157.1 £ 36-1







0
(  Pagina 2

[image: image2.png][image: image3.png][image: image4.png][image: image5.wmf]_1104730627

